## Slide 1: Solving inverse problems in crystal plasticity with differentiable programming
Fanglei Hua, Stephen Niezgodab, Tianju Xuea, Jian Caoa
a Department of Mechanical Engineering, Northwestern University
b Department of Materials Science and Engineering, The Ohio State University
Notes: 226 - Machine Learning-Based Modeling, Prediction, and Optimization in Advanced Manufacturing and Multiphysical Properties of Materials,
Zhongshu Ren, Qingchang Liu, Zhengtao Gan, Moon-ki Choi, Yue Zhang, Sourav Saha, Yu Pan, Ning Liu (https://drive.google.com/file/d/1W4XtIu279xSLR362QAhvYZVKDWgJyHDh/view)
Thank you very much for the opportunity for giving this keynote talk and summarize my recent work and my collaborators’ work for the past two years. The motivation of this work is following, you know, material properties is very microstructure-driven. And the common practice is look at the microstructure and try to predict property, right?
Now we can ask a question

## Slide 2
[1] Kaushik Bhattacharya, Learning based multi-scale modeling
ICME
Forward Mode [1]
Input Parameters
Oriented Properties
Goal-Oriented Inverse Design
Motivation
Gradient-Based Optimization
Model
Sensitivity Analysis
Initial blank geometry
Initial microstructure
Manufacturing process
…
Mechanical Properties
Desired microstructure
…
Notes: ## Integrated Computational Materials Engineering (ICME)
Here is where the forward simulation comes in. However, for smart manufacturing, what we really care about is the property. So can we actually use inverse design to design materials microstructure and/or processing path to get the property.
In this talk, the content of Inverse design means, I have a target property or several target properties as input to derive the initial blank geometry, initial microstructure, and subsequent manufacturing process parameters.

## Slide 3
Outline
Differentiable
Tool
Process
Design
Background
  Introduction of crystal plasticity (CP)
  Development of JAX-CPFEM
Easy-to-use Tool
  Calibration of CPFEM material parameters
  Material properties Mechanical properties
Material design
  Property-targeted design
  High-dimensional and gradient-based optimization
Process design
  Property-targeted design
  Multi-scale simulation: PF-CP
Calibration
Material
Design
Notes: ## Integrated Computational Materials Engineering (ICME)
Talke more examp.
Box

## Slide 4
[1] F. Zhao et al., Physical Review Letter, 116, 075501 (2016)
Crystal plasticity
Cartoon of slip and twinning deformations in a face-centered cubic (FCC) crystal [1]
Twinning plane
A mirror image
Dislocations glide
Crystal planes
Plastic Deformation
Notes: ### Introduction of CP
Undeformed grain

## Slide 5
[1] Roters, F. et al., Computational Materials Science, 2019. 158: p. 420-478.
[2] Marin, E.B., 2006, Sandia National Laboratories, Albuquerque, NM, and Livermore, CA
Crystal plasticity finite element method (CPFEM)
Constitutive Models [1]
Crystal Plasticity FEM
Self-hardening laws
Self and latent hardening laws
Momentum Balance Laws [2]
in
on
on
Div P = 0
u = uD
Pn = t
[100]
[010]
[001]
Slip / Twinning Modes
Slip rate for slip system
Rate of slip resistance
Reference slip rate
h0 Hardening parameter
gsat Saturation slip resistance …
Finite Element Method
Kalidindi’s self and latent hardening law
Notes: ### Introduction of CPFEM
Note: single crystal Ta under compression (Mesh: 5x5x5)
Backup 1: Kalidindi’s constitutive law P34

## Slide 6
$$$
Popular commercial software
Can we design a generic CPFEM software:
Easy-to-use
Affordable
Modular code
Existing open-source software
Let’s go open-sourcing!
For-loops & MPI
Tools
AutoDiff of constitutive law
GPU-accelerated
Differentiable
Notes: Font-size
WARP3D  UIUC

## Slide 7
[1] Xue, Tianju, et al., Computer Physics Communications, 291 (2023): 108802.
[2] Hu, F., Niezgoda, S., Xue, T., & Cao, J. (2025). npj Computational Materials, 11(1), 46.
What is JAX-FEM and JAX-CPFEM
Based on JAX (by Google)
  CPU/GPU compatible
  ~10× to 100× boost in performance from CPU to GPU
Implemented with pure Python
  Just-in-time compilation
  Fast developing and easy collaboration
Automatic linearization for nonlinear problems
  Work directly with the weak form
  Perform the linearization using AD
Allows end-to-end automatic differentiation (AD)
  Gradient-based design and optimization
  Full access to JAX machine learning functions
Initial version released by Google in 2018
JAX-FEM: A differentiable GPU-accelerated 3D finite element solver [1]
JAX-CPFEM: Efficient differentiable GPU-computing [2]
GitHub page
Launched in late 2024
Notes: we would like to use JAX
The package that we develop for this is called JAX-FEM.
This software is differentiable. We are using the JAX, which is a Google library for the user for Machine learning.
Automatic differentiation
Push this next level

## Slide 8
Clockwise loop of calculations during stress determination [1]
At (n+1) time step, mapping Fn+1 to Sn+1
Elastic Deformation
Gradient
Second Piola-Kinchhoff
Stress
Div P = 0 in , where
    Newton-Raphson Method
    is not explicitly a function of
    Newton-Raphson Method
[1] Roters, F. et al., Computational Materials Science, 2019. 158: p. 420-478.
Char. 1: AutoDiff of constitutive laws
Governing Equation
Constitutive Laws
Plastic Deformation
Gradient
Plastic Velocity
Gradient
Notes: ### Easy to use

## Slide 9
Clockwise loop of calculations during stress determination [1]
At (n+1) time step, mapping Fn+1 to Sn+1
Elastic Deformation
Gradient
Second Piola-Kinchhoff
Stress
    Newton-Raphson Method
Char. 1
Constitutive Laws
Plastic Deformation
Gradient
Plastic Velocity
Gradient
,
CP slip derivative [1]
Automatic Differentiation (AD) for Jacobian matrix:
  Different constitutive laws
  Different physics mechanisms
  Whenever there is derivative to evaluate
[1] https://mooseframework.inl.gov/source/materials/crystal_plasticity/
AutoDiff of constitutive law: jax.jacfwd

## Slide 10
Char. 2: GPU-acceleration
CPU/GPU compatible:
  Array programming – jax.vmap
  Just-in-time compilation – jax.jit
  Matrix formulation – constitutive laws
Slip resistance
[1] Hu, F., Niezgoda, S., Xue, T., & Cao, J. (2025). npj Computational Materials, 11(1), 46.
(~1d)
(~0.6 h)
Notes: We compare it with the another open source code MOOSE. It matched pretty well.
And the time that we have is lots of advantages when you have more degrees of freedom
So five by five by five, it is probably computational time very similar. But once you go beyond, more and more, as you can see, JAX-CPFEM is down here.
JAX-CPFEM (CPU / GPU) is 12.8× / 39.0× faster than MOOSE (CPU MPI 8) for the 52.7 thousand degree of freedoms problem [1]

## Slide 11
Char. 3: Automatic sensitivity
Ensured Grain Orientations – Copper (0.1mm) – 100 grains
g0 gss_initial (60.8) Initial slip resistance
a gss_a (2.5) Hardening parameter
h0 h (541.5) Hardening parameter
gsat t_sat (109.8) Saturation slip resistance
n xm (0.1) Rate sensitivity exponent
,
Kalidindi’s constitutive model
Material parameters:
Effect of on () at different stages (
AutoDiff & Implicit Diff.
Notes: ## Differentiable

## Slide 12
[1] Fanglei Hu, et al., TMS Specialty Congress 2024
 | [ s-1 ] | a [ - ] | h0 [ - ] | gsat [ MPa ] | n [ - ]
AD 1225s @M2 | 16527.3 | -9.8 | 4.0 | 15.1 | 2538.6
FDM (1e-4) 7775s @M2 | 16527.3 | -9.8 | 4.0 | 15.2 | 2538.6
 |  | a [ - ] | h0 [ - ] | gsat [ MPa ] | n [ - ]
AD 1225s @M2 | 16527.3 | -9.8 | 4.0 | 15.1 | 2538.6
FDM (1e-4) 7775s @M2 | 16527.3 | -9.8 | 4.0 | 15.2 | 2538.6
Note: JAX-CPFEM: AD (CPU @ M2) is 6.3× faster than FDM (CPU @ M2)
Finite Difference Method (FDM)
Char. 3: Automatic sensitivity
Note: 0.001%~0.3% difference between AD and FDM

## Slide 13
[1] Hu, F., Niezgoda, S., Xue, T., & Cao, J., to be submitted
[2] Hu, F., Niezgoda, S., Xue, T., & Cao, J. (2025). npj Computational Materials, 11(1), 46.
[3] Unpublished results
Brief summary of JAX-CPFEM
AutoDiff of Constitutive Laws
  Free to realize different deformation mechanics
  Case-by-case Jacobian matrix
GPU-acceleration
  Efficient solution to forward CPFEM
  array programming style
  matrix formulation
Automatic Sensitivity
  Sensitivity analysis with respect to design parameters
  Integrated with inverse design seamlessly
Three features of differential JAX-CPFEM
JAX-CPFEM
Process
Design
Calibration
Material
Design
GitHub page
Notes: Note: ～17 mins
We want to emphasize the following three features that differential JAX-CPFEM differ from other CPFEM software:
Automatic Constitutive Laws: Free to realize different deformation mechanics represented by constitutive materials laws by evaluating the case-by-case Jacobian matrix using automatic differentiation.
Automatic Sensitivity: Differential simulation for sensitivity analysis with respect to design parameters used in single crystal or polycrystal, which can be seamlessly integrated with inverse design.
GPU-acceleration: Efficient solution to forward CPFEM (involving complicated nonlinear relations) with GPU acceleration based on array programming style and matrix formulation.

## Slide 14
Outline
JAX-CPFEM
Process
Design
Background
  Introduction of crystal plasticity
  Development of JAX-CPFEM
Easy-to-use Tool
  Calibration of CPFEM material parameters
  Material properties Mechanical properties
Material design
  Property-targeted design
  High-dimensional and gradient-based optimization
Process design
  Property-targeted design
  Multi-scale simulation: PF-CP
Calibration
Material
Design
GitHub page
Notes: Calibration of CPFEM material parameters by multi-objective optimization with AD‐based sensitivities

## Slide 15
Crystal Plasticity
Finite Element Method
(CPFEM)
Input Parameters
Output
Properties
h0 Hardening parameter
n Rate sensitivity exponent
gsat Saturation slip resistance
……
Stress-Strain Curve
Yield Stress
Hardening Rate
……
Forward Mode
“Back propagation” for inverse analysis
Objective Function
PDE-CO problem
Minimize the misfit between the CPFEM simulations and experimental data
Calibration of material parameters
Notes: Similar figures

## Slide 16
[1] Depriester et al., International Journal of Plasticity, 2023. 168: p. 103695. [2] A. Tran et al., Computational Mechanics, 2023. 1-14.
[3] J. Kuhn et al., Optimization and Engineering, 2021. 1-35. [4] K. Sedighiani, et al., Mechanics of Materials, 2022. 104117.
[5] Chakraborty et al., European Journal of Mechanics-A/Solids, 2017. 66: p. 114-124
  In-situ Mechanical Test / Characterization [1]
    Actual properties of single crystals
    Expensive & time-consuming
  Trial-And-Error
    Fitting of mechanical data
    Fitting of microscopic material models
Reconstructed grains from EBSD characterization
Aim：Get CPFEM constitutive parameters accurately and efficiently？
Calibration of material parameters
  Gradient-Free (GF) Optimization
    Bayesian optimization [2][3]
    Genetic algorithm [4]
    Nelder-Mead algorithm [5]
Gradient-Based (GB) inverse optimization？
Notes: ## Backup3 calibration pipeline
This is where the JAX-CPFEM come in.
Nano-indetor

## Slide 17
[1] Tran et al., 2023, AIAA SCITECH 2023 Forum.
CPFEM
Input Parameters
Output
Properties
Forward Mode
Material Parameters [1]
Stress-Stain Curve
Kalidindi’s self and latent hardening laws
Gradient backpropagation
(1) g0 (90.0) Initial slip resistance
(2) a (8.0) Hardening parameter
(3) h0 (392.977) Hardening parameter
(4) gsat (7295.1754) Saturation slip resistance
(5) n (1.0/120.0) Rate sensitivity exponent
(6) r (1.0) Interaction coefficient
Loading along z-axis or x-axis
Scenario 1
Scenario 2
Reference result
Case study: reference
Notes: ## Backup 3: GB calibration results - Dual phase P37

## Slide 18
[1] Byrd et al., SIAM Journal on Scientific and Statistical Computing, 1995.16 (5): 1190-1208.
[2] Hu, F., Niezgoda, S., Zha, R., Xue, T., & Cao, J., to be submitted
Case study: GB calibration results
.
-- verified.
Gradient-based Optimization
L-BFGS-B algorithm [1] for Gradient-based optimization:
  Bound-constrained minimization
  SciPy package 1.11.1
Objective values vs. No. of calls [2]
Stress-Strain curve before and after calibration [2]
Match
Notes: ## Backup 3: GB calibration results P36

## Slide 19
Calibration: GB vs GF - Efficiency
Comparing Gradient-based and Gradient-free Optimizations [1]
Bayesian algorithm for gradient-free optimization
  Same initial guess and guess range of parameter
  Scikit-optimize package 0.9.0
Conclusions:
Approximately 7× fewer iterations
A 3× to 4× efficiency improvement
[1] Hu, F., Niezgoda, S., Zhou, R., Ryou K., Dunand D., Zha, R., Xue, T., & Cao, J., to be submitted
Notes: Forward calls

## Slide 20
Comparing Gradient-based and Gradient-free Optimizations [1]
Bayesian algorithm for gradient-free optimization
  Same initial guess and guess range of parameter
  Scikit-optimize package 0.9.0
Calibration: GB vs GF - Accuracy
Comparison between the reference result and calibrated results of single-crystal copper obtained from gradient-based and gradient-free optimizations (five tests).
[1] Hu, F., Niezgoda, S., Zhou, R., Ryou K., Dunand D., Zha, R., Xue, T., & Cao, J., to be submitted
Notes: ## Backup 4: GO scenario
matrics

## Slide 21
Application to Wrought IN625
Calibration
[1] Hu, F., Niezgoda, S., Zhou, R., Ryou K., Dunand D., Zha, R., Xue, T., & Cao, J., to be submitted
  Homogenized at 1150 for 3 hours
  Area-weighted mean grain size of 14752
Inverse pole figure (IPF) maps
Comparison between the experimental result and calibrated results
Notes: ## Backup 4: GO scenario ~23 min

## Slide 22
Outline
JAX-CPFEM
Process
Design
Background
  Introduction of crystal plasticity
  Development of JAX-CPFEM
Easy-to-use Tool
  Calibration of CPFEM material parameters
  Material properties Mechanical properties
Material design
  Property-targeted design
  High-dimensional and gradient-based optimization
Process design
  Property-targeted design
  Multi-scale simulation: PF-CP
Calibration
Material
Design
Notes: Case Study 1: Property-targeted microstructure/material design

## Slide 23
[1] Hu, F., Niezgoda, S., Xue, T., & Cao, J. (2025). Efficient GPU-computing simulation platform JAX-CPFEM for differentiable crystal plasticity finite element method. npj Computational Materials, 11(1), 46.
GitHub page
Launched in late 2024
Euler Angle Z-Y-X
Initial Guess
Euler Angle
Euler Angle
Euler Angle
Designed Results
m-3m
[101]
[001]
[111]
z
y
x
Materials design
Notes: ~1.18 hours (4231 secs) for 32 iterations on DM GPU @ RTX 8000. ~26min
Let’s see you know, I have the material and I really want to have certain yield stress and I also really want to have certain energy absorption capability.
This is where the desired stress-strain curve comes in. If you wan to have this one, the dotted one, what is the microstruture you need to give you that behavior, right? So you can start with Euler angle with very constant ones across this grid. And each one, if you do the inverse pole figure, which is here. And it’s a red line.
So the question is can we find out the microstructure that will give us this dotted line, which we basically use JAX-CPFEM and put the optimization, and after you run around 31 iterations. You can see that each cell at that block is actually giving you different phase. So it ends up with this final microstructure.

## Slide 24
Outline
JAX-CPFEM
Process
Design
Background
  Introduction of crystal plasticity
  Development of JAX-CPFEM
Easy-to-use Tool
  Calibration of CPFEM material parameters
  Material properties Mechanical properties
Material design
  Property-targeted design
  High-dimensional and gradient-based optimization
Process design
  Property-targeted design
  Multi-scale simulation: PF-CP
Calibration
Material
Design
Notes: Case Study 2: Process path design

## Slide 25
Property-targeted process design
[1] Sedighiani, Karo, et al. Acta Materialia 237 (2022): 118167.
[2] Yilmaz, Fatih, et al. The International Journal of Advanced Manufacturing Technology (2025): 1-21.
Crystal Plasticity
Finite Element Method
(CPFEM)
Input Parameters
Cold Rolling Process
Time-dependent applied displacement
Forward Mode
“Back propagation” for inverse analysis
Objective Function
PDE-CO problem
Initial Microstructure
Grain size, Orientation distribution…
Output Properties
Mechanical Property
Stress/Strain status, Yield stress, …
[1][2]
Multi-Path rolling

## Slide 26
[1] Kovachki, Nikola, et al. Mechanics of Materials 165 (2022): 104156. [2] Han, Zhiqiang, et al. Computational Materials Science 101 (2015): 248-254.
[3] Yeddu, et al. Acta Materialia 102 (2016): 97-107. [4] Staublin, Philip, et al. Acta Materialia 237 (2022): 118169.
[5] Dantzig, J. A., et al. Metallurgical and Materials Transactions A 44 (2013): 5532-5543.
[6] Xue, Tianju, et al., Computer Methods in Applied Mechanics and Engineering 385 (2021): 114046.
Finite Element
Crystal Plasticity
Phase Field
Dislocation Dynamics
Molecular Dynamics
DFT
Input Parameters
Oriented Properties
Initial blank geometry
Initial microstructure
Manufacturing process
…
Mechanical Properties
Desired microstructure
…
Some Applications:
Precipitation [2]
Martensite [3]
[1]
Grain Growth [4]
Dendritic Growth [5]
Fracture [6]
Property-targeted process design
Notes: Version 2

## Slide 27
3D printing products
  Highly Anisotropic
  PF: Processing – Microstructure
Phase-field modeling of microstructure evolution during 3D printing [1][2]
Uniaxial tensile deformation of a 0.0433 mm3 304 steel
Degrees of Freedom: 213* 3 = 27,783 Dofs No of Grain: 19
[1] Choi, Jin Young, et al., Additive Manufacturing 79 (2024): 103938.
[2] Xue, Tianju, et al. npj Computational Materials 8.1 (2022): 201.
Post-Processing of 3D printing products
  Highly Anisotropic
  CP: Microstructure – Property
CPFEM
Property-targeted process design
Notes: [1] PF provides microstructure of 3D printing product, what is the post-processing?
[2] An inverse problem
Jin surrogate

## Slide 28
Apply strain that varies nonlinearly
with respect to time
Targeted mechanical properties vs. applied strain
along x-axis
Forward Mode
“Back propagation”
for inverse design?
ux (t) uy (t)
Biaxial tensile deformation of a 0.02 mm FCC polycrystal 304 steel
Design Space
Property-targeted process design
Notes: Cut off Case 1
Bai-axiail

## Slide 29
[1] Unpublished results
L-BFGS-B gradient-based optimization
234 iterations
62.6h (GPU)
3,993 DoFs
102 Designed Variables
Objective values vs. No. of calls
Reference vs. Designed variables during iterations
Property-targeted process design
Notes: IF you want to have this kind of stress strain curve behavior, what is the loading pass?
You can do the inverse analysis, and then you can that you start this one and actually can calculate the strain path for you

## Slide 30
The central goal is to facilitate inverse design in manufacturing.
Multi-GPU/CPU version for large size problem
(~1 million DoF for a single GPU )
We are building a platform to do multi-physics and multi-scale simulation (computational material science).
Theme of Our Work
Differentiable
Tool
Process
Design
Calibration
Material
Design
GitHub page
Notes: 1. Limitation of memory
2. Multi-physics
3. multi-scale – Phase transformation

## Slide 31
Acknowledgements
We would like to acknowledge support from the Department of Defense Vannevar Bush Faculty Fellowship, USA N00014-19-1-2642, and from the NSF Engineering Research Center for Hybrid Autonomous Manufacturing Moving from Evolution to Revolution (ERC‐HAMMER) under Award Number EEC-2133630.
Notes: Backup: Performance P33
Backup 1: Kalidindi’s constitutive law P34
Backup 2: Automatic sensitivity P35
Backup 3: GB calibration results P36
Backup 3: GB calibration results - Dual phase P37
Backup 4: AutoDiff of constitutive laws P38
Backup 5: Microstructure-targeted process design P39
Backup 7: Phase field model P45

## Slide 32: Backup
Notes: ##

## Slide 33
JAX-CPFEM (CPU)
2.3 GHz Intel(R) Xeon(R) W-2195 CPU (18 cores) with NVIDIA Quadro
RTX 8000 GPU (48 GB Graphics memory) on Ubuntu 20.04.5 LTS.
MOOSE (CPU MPI 8 cores)
2.3 GHz Intel(R) Xeon(R) W-2195 CPU (18 cores)
Hardware and operating system
Backup: Performance

## Slide 34
Kinematic Formalism
Governing Equation
Momentum Balance
Div P = 0
u = uD
Pn = t
P First Piola-Kirchhoff stress
S Second Piola-Kirchhoff stress
F Deformation Gradient
in
on
on
Constitutive Model
Phenomenological constitutive model
Physics-based constitutive model
Plastic velocity gradient
Sum of contributions
from all slip systems
Slip rate for slip system
Rate of slip resistance
Reference slip rate
h0 Hardening parameter
gsat Saturation slip resistance …
Backup 1: Kalidindi’s constitutive law

## Slide 35
[1] Fanglei Hu, et al., TMS Specialty Congress 2024
 |  | a | h0 | gsat | n
AD 1225s (M2) | 16527.3 | -9.8 | 4.0 | 15.1 | 2538.6
FDM (1e-4) 7775s (M2) | 16527.3 | -9.8 | 4.0 | 15.2 | 2538.6
 |  | a | h0 | gsat | n
AD 1225s (M2) | 16527.3 | -9.8 | 4.0 | 15.1 | 2538.6
FDM (1e-4) 7775s (M2) | 16527.3 | -9.8 | 4.0 | 15.2 | 2538.6
 |  | a | h0 | gsat | n
AD | 24353.6 | -34.3 | 17.0 | 52.8 | 4334.4
FDM | 24352.8 | -34.2 | 17.0 | 52.9 | 4334.4
 |  | a | h0 | gsat | n
AD | 24353.6 | -34.3 | 17.0 | 52.8 | 4334.4
FDM | 24352.8 | -34.2 | 17.0 | 52.9 | 4334.4
Note: JAX-CPFEM: AD (CPU @ M2) is 6.3× faster than FDM (CPU @ M2)
Finite Difference Method (FDM)
Backup 2: Automatic sensitivity
Note: 0.001%~0.3% difference between AD and FDM
Notes: Box for time
Units
Incre.
Just 1 as example
Put the time out

## Slide 36
Backup 3: GB calibration results
Gradient-based Optimization
Material Parameters |  | Misfit between stress values:
Initial slip resistance g0 [MPa] | Ref. value | 1.0 90.0
 | Calib. value | 0.997898 90.0
 | Diff. | 0.210%
Hardening parameter a | Ref. value | 1.0 8.0
 | Calib. value | 2.209654 8.0
 | Diff. | 120.965%
Hardening parameter h0 | Ref. value | 1.0 392.9772
 | Calib. value | 1.066548 392.9772
 | Diff. | 6.655%
Material Parameters |  | 
Initial slip resistance g0 [MPa] | Ref. value | 
 | Calib. value | 
 | Diff. | 0.210%
Hardening parameter a | Ref. value | 
 | Calib. value | 
 | Diff. | 120.965%
Hardening parameter h0 | Ref. value | 
 | Calib. value | 
 | Diff. | 6.655%
Material Parameters |  | Misfit between stress values:
Saturation slip resistance gsat [MPa] | Ref. value | 1.0 7295.1754
 | Calib. value | 1.053586 7295.1754
 | Diff. | 5.359%
Rate sensitivity exponent n | Ref. value | 1.0 (1.0/120.0)
 | Calib. value | 1.040702 (1.0/120.0)
 | Diff. | 4.070%
Interaction coefficient r | Ref. value | 1.0 1.0
 | Calib. value | 1.066548 1.0
 | Diff. | 6.655%
Material Parameters |  | 
Saturation slip resistance gsat [MPa] | Ref. value | 
 | Calib. value | 
 | Diff. | 5.359%
Rate sensitivity exponent n | Ref. value | 
 | Calib. value | 
 | Diff. | 4.070%
Interaction coefficient r | Ref. value | 
 | Calib. value | 
 | Diff. | 6.655%
Ill-posed problem:
  Close to their reference values within 8% difference (Acceptable)
Ref. value:;
Calib. value:;
.